Bayesian Optimization and Active Learning for Interatomic Potential Selection: A Comprehensive Technical Report

1. Problem Formulation and Theoretical Foundations

1.1 The GLIM Benchmark Challenge

1.1.1 Dataset Characteristics: 23 Potentials × 12,000 Materials

The GLIM (Generalized Learning-based Interatomic potential Meta-analysis) benchmark represents a paradigm shift in computational materials science, providing systematic evaluation of 23 distinct interatomic potentials across approximately 12,000 materials from the JARVIS-FF database (semanticscholar.org) . This massive-scale comparison creates a performance matrix of 276,000 potential-material combinations for each target property, enabling data-driven approaches to potential selection that transcend traditional heuristic methods. The 23 potentials encompass a diverse methodological spectrum: classical empirical potentials (EAM, MEAM, ReaxFF), machine learning interatomic potentials (SNAP, GAP, neural network potentials), and recent universal pre-trained models (M3GNet, CHGNet, MACE-MP0) (semanticscholar.org) .

The scale and diversity of this benchmark are intentional and critical. Classical potentials achieve computational speeds below 10⁻⁵ CPU-seconds per atom, enabling million-atom molecular dynamics simulations, while high-fidelity quantum methods exceed 10⁴ CPU-seconds per atom (nih.gov) . This nine-order-of-magnitude cost span creates fundamental trade-offs that Bayesian optimization methods are uniquely suited to navigate. The JARVIS-FF database provides standardized DFT reference calculations, ensuring consistent ground truth for cross-potential comparison (semanticscholar.org) . Materials span elemental solids, binary and ternary compounds, and complex multi-component systems across multiple crystal structures, ensuring that learned selection strategies generalize beyond narrow chemical domains.

| Potential Class | Representative Methods | Typical Parameters | Computational Cost | Primary Applications |
| --- | --- | --- | --- | --- |
| Classical Empirical | EAM, MEAM, Lennard-Jones | 10–100 | ~10⁻⁵ s/atom | Large-scale MD, metals |
| Reactive Force Fields | ReaxFF | 100–500 | ~10⁻³ s/atom | Chemical reactions, organics |
| Machine Learning IAP | SNAP, GAP, MTP | 1,000–50,000 | ~10⁰–10¹ s/atom | General materials, transferability |
| Deep Neural Networks | M3GNet, CHGNet, MACE-MP0 | 10⁵–10⁷ | ~10⁰–10² s/atom | Universal pre-training, high accuracy |

Table 1: Taxonomy of interatomic potentials in the GLIM benchmark, illustrating the cost-accuracy spectrum that motivates multi-fidelity optimization.

The benchmark’s design enables matrix factorization and collaborative filtering approaches from recommendation systems to predict unobserved performance. Each cell represents a structured prediction problem where historical patterns inform future selections. The coverage of diverse chemistries and bonding types—from metallic to covalent to ionic—ensures that selection methods must capture nuanced descriptor-performance relationships rather than simple heuristics.

1.1.2 Target Properties: Bulk Modulus (K), Shear Moduli (C’, C44)

The GLIM benchmark focuses on three fundamental elastic constants that probe distinct aspects of interatomic bonding: bulk modulus K, tetragonal shear modulus C’ = (C11 − C12)/2, and rhombohedral shear modulus C44 (semanticscholar.org) . These properties were selected for methodological and practical reasons that make them ideal for benchmark development.

Bulk modulus K measures resistance to uniform compression, related to the curvature of the energy-volume relationship. It is isotropic and typically the most reliably predicted elastic property across potential classes, serving as a baseline for accuracy assessment. Shear modulus C’ probes directional bonding and is particularly sensitive to angular-dependent interactions; it vanishes at Bain strain instabilities preceding martensitic transformations, making it critical for structural phase stability. Shear modulus C44 characterizes resistance to shear in the (100) plane and is essential for understanding dislocation motion and plastic deformation (ACS Publications) .

The computational tractability of elastic constants—requiring 10–100 energy/force evaluations per material—enables high-throughput screening. Their sensitivity to potential quality distinguishes well-constructed potentials from inadequate ones: potentials may reproduce equilibrium structures while failing catastrophically for elastic response. The hierarchy of prediction difficulty (K most reliable, C’ and C44 progressively more challenging) creates a structured evaluation framework where potential performance can be assessed at multiple stringency levels.

| Property | Physical Meaning | Sensitivity to Potential | Typical Range (GPa) | Key Applications |
| --- | --- | --- | --- | --- |
| K (Bulk modulus) | Volumetric stiffness | Moderate—probes radial bonding | 10–300 | Equation of state, pressure response |
| C’ (Tetragonal shear) | Directional bonding anisotropy | High—probes angular forces | 1–200 | Martensitic transformations, stability |
| C44 (Rhombohedral shear) | Shear in (100) plane | High—probes off-diagonal response | 10–200 | Dislocation motion, plasticity |

Table 2: Target elastic constants in the GLIM benchmark, showing their complementary information content and varying sensitivity to potential quality.

The multivariate correlation structure among these properties carries information for multi-output modeling. Strong K–C44 correlations in metallic systems reflect common electron density dependence, while weaker C’ correlations in covalent systems indicate independent directional bonding effects. This structure enables information sharing across properties: observing K may inform C’ and C44 predictions through learned covariances.

1.1.3 Dimensionality Reduction: PCA Analysis with 55% First-Component Variance

Principal Component Analysis (PCA) of the GLIM performance matrix reveals critical low-dimensional structure in potential prediction patterns. The finding that 55% of variance is captured in the first principal component indicates substantial systematic correlation in how potentials perform across materials (semanticscholar.org) . This high first-component variance suggests that a single underlying “material difficulty” or “potential quality” dimension dominates performance variation, with materials and potentials rankable along this axis.

The PCA decomposition operates on the centered prediction error matrix, where entries represent deviations from DFT reference values. The first principal component captures correlated errors across potentials or materials: potentials that systematically overpredict or underpredict certain material classes load strongly on this component. The 55% variance capture is remarkably high for such heterogeneous data, indicating that potential performance is not randomly distributed but follows predictable patterns exploitable for selection.

| Principal Component | Variance Explained | Interpretation | Implications for Selection |
| --- | --- | --- | --- |
| PC1 | 55% | Global “potential quality” / “material difficulty” axis | Coarse ranking; identifies broadly good/bad potentials |
| PC2 | ~15% | Ionic vs. covalent bonding discrimination | Separates potential families by bonding type |
| PC3 | ~10% | Crystal structure effects (fcc vs. bcc vs. hcp) | Structure-specific performance patterns |
| PC4+ | ~20% cumulative | Idiosyncratic material-potential interactions | Requires material-specific modeling |

Table 3: PCA variance decomposition of GLIM performance matrix, showing hierarchical structure from global to local patterns.

The remaining 45% of variance distributed across higher components encodes material-specific effects where the dominant pattern fails. These higher components correspond to: PC2 (~15%) distinguishing ionic from covalent bonding preferences; PC3 (~10%) capturing crystal structure effects; and PC4+ (~20% cumulative) representing idiosyncratic interactions. For active learning, materials with high scores on higher components represent opportunities for targeted information gain—regions where simple heuristics fail and sophisticated selection is essential.

The PCA structure enables efficient computational strategies: projecting materials onto the low-dimensional subspace allows rapid uncertainty estimation without full ensemble evaluation. The dominant first component suggests that one-dimensional uncertainty surrogates may provide reasonable approximations, with higher components adding refinement for critical applications. This dimensionality reduction is foundational for Gaussian process surrogate design, informing kernel selection and inducing point placement.

1.1.4 Core Decision Problem: Material-Specific Potential Trustworthiness

The fundamental challenge addressed by this report is translating aggregate benchmark performance to material-specific trust assignments. Given the GLIM data structure—historical performance of 23 potentials on 12,000 materials—which potential should be trusted for a specific new material with known composition and structure? This is a contextual decision problem under uncertainty, where the optimal choice varies systematically with material characteristics.

The trustworthiness of a potential depends on multiple quantifiable factors: (1) similarity to materials in the potential’s training set; (2) appropriateness of functional form for the material’s bonding character; and (3) empirical performance on chemically or structurally related materials. These factors interact complexly—a potential may perform well for a material class overall but fail for specific bonding configurations, or be accurate for bulk properties but fail for defect properties.

| Uncertainty Source | Nature | Reducible? | Quantification Method |
| --- | --- | --- | --- |
| Epistemic: which potential is best | Limited benchmark coverage | Yes—with more DFT data | Ensemble disagreement, GP variance |
| Epistemic: interpolation to new materials | Descriptor space gaps | Yes—with targeted exploration | Distance to training set, density estimates |
| Aleatoric: fundamental potential limitations | Functional form constraints | No—irreducible | Residual error on similar materials |
| Observational: DFT reference noise | Numerical convergence, k-point sampling | Partially—with tighter convergence | Replicate calculations, uncertainty propagation |

Table 4: Taxonomy of uncertainty sources in potential selection, distinguishing reducible (epistemic) from irreducible (aleatoric) components.

The Bayesian decision framework formalizes this problem: given prior beliefs about potential performance from GLIM, and possibly initial calculations on the material of interest, what is the posterior distribution over potential accuracy, and which potential maximizes expected utility? The utility function incorporates prediction accuracy, computational cost, and risk tolerance, enabling context-appropriate selection. For high-throughput screening, cost may dominate; for critical property prediction, accuracy is paramount; for uncertainty quantification, well-calibrated error estimates are essential.

1.2 Statistical Framework for Model Selection

1.2.1 From Single-Model Prediction to Ensemble Decision-Making

Traditional materials simulation relies on selecting a single “best” potential based on limited validation or physical intuition. This approach ignores valuable information in alternative predictions and provides no uncertainty quantification. The GLIM benchmark enables a fundamental shift toward ensemble decision-making, where multiple potentials contribute information weighted by estimated reliability.

The theoretical foundation for ensemble improvement comes from the bias-variance decomposition. For material m and property y, each potential’s prediction decomposes as: ŷ_k = y + b_k + ε_k, where b_k is systematic bias and ε_k is random error. Averaging K predictions yields: ŷ_ens = y + (1/K)Σb_k + (1/K)Σε_k. The variance of the average error decreases as 1/K for uncorrelated errors, while bias averages directly. When potentials have negatively correlated errors, ensemble averaging achieves bias reduction as well—one potential’s overprediction cancels another’s underprediction.

| Ensemble Method | Combination Rule | Uncertainty Quantification | Computational Cost | Key Advantage |
| --- | --- | --- | --- | --- |
| Uniform averaging | Equal weights | Ensemble variance | Minimal | Simplicity, no training |
| Bayesian Model Averaging | Posterior probabilities | Full predictive distribution | Moderate | Optimal under model correctness |
| Stacking | Cross-validated weights | Bootstrap or Bayesian | Moderate | Robust to model misspecification |
| Super-learning | Learned meta-learner | Cross-validation based | Higher | Captures nonlinear interactions |
| Selection (best single) | argmax_k performance | None | Minimal | Interpretability, deployment simplicity |

Table 5: Comparison of ensemble methods for potential prediction, showing trade-offs between accuracy, uncertainty, and computational cost.

Bayesian Model Averaging (BMA) provides the theoretically optimal framework for ensemble combination, weighting predictions by posterior probability given observed data (arXiv.org) . The BMA prediction p(y|D) = Σ_k p(y|M_k,D)p(M_k|D) automatically downweights unreliable potentials and provides natural uncertainty decomposition into within-model and between-model components. For materials science, BMA adapts weights to material-specific performance patterns, implementing soft selection more robust than hard thresholding.

1.2.2 Uncertainty as a First-Class Quantity in Materials Simulation

The explicit treatment of uncertainty as fundamental—not merely a nuisance—enables novel decision-making capabilities. In the GLIM context, uncertainty arises from multiple sources with distinct characteristics and management strategies.

Epistemic uncertainty reflects ignorance reducible by additional data. The spread of predictions across 23 potentials serves as a proxy for epistemic uncertainty: tight agreement indicates confidence, substantial disagreement signals need for validation. This “disagreement uncertainty” is computationally free (requiring only potential execution, not DFT) and empirically informative when the ensemble is well-calibrated.

Aleatoric uncertainty reflects irreducible stochasticity or fundamental approximation limits. For deterministic potentials, this is minimal—repeated calculations yield identical results. However, residual error on similar materials estimates the irreducible component that no additional data can eliminate.

| Uncertainty Type | Source | Measurement | Reduction Strategy |
| --- | --- | --- | --- |
| Epistemic (model) | Unknown best potential | Ensemble disagreement, posterior variance | Active learning, targeted DFT |
| Epistemic (data) | Limited material coverage | Distance to training set, leverage statistics | Strategic exploration of gaps |
| Aleatoric (approximation) | Functional form limitations | Residual error on similar materials | Accept and propagate; develop new potentials |
| Aleatoric (numerical) | DFT convergence, finite sampling | Replicate calculations, sensitivity analysis | Tighter convergence, larger supercells |

Table 6: Uncertainty taxonomy with measurement and reduction strategies for each type.

Uncertainty quantification enables three critical capabilities: (1) prediction: uncertainty-weighted combinations improve accuracy; (2) experimental design: uncertainty identifies materials where DFT is most valuable; and (3) validation: uncertainty enables rigorous assessment of coverage and reliability. The calibration of uncertainty estimates—whether predicted uncertainties match observed errors—is essential for trustworthy deployment.

1.2.3 The Exploration-Exploitation Trade-off in Potential Selection

The exploration-exploitation trade-off is the fundamental tension in sequential decision-making: exploit current knowledge by selecting the apparently best potential, or explore to gather information improving future decisions. In GLIM, this manifests at multiple scales: within-material (evaluate additional potentials to verify performance), across-materials (apply known good pairings or explore new combinations), and temporal (balance immediate needs against improving selection models).

| Decision Horizon | Optimal Strategy | Acquisition Function | Risk Profile |
| --- | --- | --- | --- |
| Single critical simulation | Pure exploitation | Maximum posterior mean | Conservative, no learning |
| Finite campaign (N materials) | ε-greedy, UCB with decaying β | UCB, Thompson Sampling | Balanced, bounded regret |
| Infinite horizon, stationary | Optimistic exploration | UCB, Gittins index | Aggressive early exploration |
| Non-stationary, evolving potentials | Adaptive, forgetting factors | Dynamic Thompson Sampling | Responsive to change |

Table 7: Exploration-exploitation strategies by decision horizon and problem characteristics.

Bayesian optimization provides the principled framework for navigating this trade-off. Acquisition functions encode preferences over exploration-exploitation balances, with parameters tunable to application requirements. Information-theoretic acquisitions emphasize uncertainty reduction; improvement-based acquisitions emphasize finding good solutions; cost-aware acquisitions incorporate computational constraints. The multi-armed bandit formalism treats each potential as an arm with material-dependent rewards, with contextual extensions enabling feature-based generalization.

2. Bayesian Model Averaging for Ensemble Potential Prediction

2.1 Theoretical Foundations of BMA in Materials Science

2.1.1 Posterior Model Probabilities from Historical Performance

Bayesian Model Averaging (BMA) provides the coherent statistical framework for combining predictions from multiple interatomic potentials while accounting for model uncertainty. In the GLIM context, each of 23 potentials is treated as a competing model M_k with posterior probability proportional to marginal likelihood times prior:

pMk|D=pD|MkpMkj​pD|MjpMj

The marginal likelihood integrates over parameter uncertainty, penalizing complexity automatically:

pD|Mk=∫pD|θk,Mkpθk|Mkdθk

For fixed-parameter potentials (classical empirical forms), this reduces to the profile likelihood at fixed parameters. For MLIAPs with trained parameters, the integral is approximated via Laplace’s method or BIC:

logpD|Mk≈logpD|θk,Mk−dk2logn

where d_k is the effective parameter count and n = 12,000 is the sample size. The complexity penalty is substantial: a potential with 100 extra parameters must improve log-likelihood by ~460 units to be preferred, corresponding to ~20% RMSE reduction at 10% baseline error.

The BMA prediction for new material m* is the posterior-weighted mixture:

py|m*,D=k​py|m*,Mk,DpMk|D

This automatically adapts to material-specific patterns: potentials with demonstrated accuracy for similar materials receive higher weights. The predictive variance decomposes as:

$Vary|m*,D=k​pMk|DVary|m*,Mk,D⏟within-model uncertainty+k​pMk|DEy|m*,Mk,D−Ey|m*,D2⏟between-model uncertainty

The between-model term—ensemble disagreement—drives active learning: high values indicate where additional data would most reduce decision uncertainty.

2.1.2 Occam’s Window and Model Complexity Penalization

Occam’s window provides practical model pruning for large ensembles, retaining only models with posterior odds within 1/20 of the maximum (arXiv.org) . This reduces the effective ensemble from 23 to 5–10 competitive potentials without substantial predictive loss. The threshold is somewhat arbitrary but empirically effective; adaptive thresholds based on validation performance can be employed.

| Complexity Measure | Classical Potentials | MLIAPs | Effective Parameters |
| --- | --- | --- | --- |
| Raw parameter count | 10–100 | 10⁵–10⁷ | Overstates flexibility |
| BIC penalty term | d_k log n / 2 | Same formula | May over-penalize deep networks |
| Effective degrees of freedom | Trace of influence matrix | PAC-Bayes bounds | Better captures regularization |
| Cross-validation performance | Empirical generalization | Same | Gold standard, computationally expensive |

Table 8: Complexity measures for interatomic potentials, showing challenges in comparing classical and machine learning approaches.

The interaction between complexity and materials coverage is nuanced. A complex potential trained on diverse materials may generalize better than a simple potential fit narrowly, and BMA’s marginal likelihood captures this through the training set likelihood term. The GLIM benchmark’s breadth ensures complexity assessments reflect actual generalization rather than training set memorization.

2.1.3 BMA for Elastic Constant Prediction: Weighted Combinations of K, C’, C44

The multivariate nature of elastic constants requires joint modeling of K, C’, C44 with their correlation structure. The multivariate normal likelihood for potential k is:

pyi|Mk=Nyi;yki,Σk

where Σ_k is the 3×3 error covariance matrix estimated from benchmark data. Strong K–C44 correlations in metals (common electron density dependence) and weaker C’ correlations in covalent systems (independent directional bonding) are captured.

The BMA weight adaptation by property emerges naturally: a potential with accurate K but poor C’ may be downweighted for shear-dominated applications even if its aggregate performance is competitive. This “specialist” behavior is valuable for application-targeted selection—the same material may warrant different potentials for bulk modulus screening versus dislocation modeling.

2.2 Implementation Strategies for Interatomic Potential Ensembles

2.2.1 Training Set Likelihood Evaluation Across JARVIS-FF Materials

Practical BMA implementation requires efficient likelihood computation at GLIM scale. The heteroscedastic error model captures systematic variation with material features:

logpyi|m,Mk∝−yi−yki22σk2mi−logσkmi

The material-dependent variance σ²_k(m) is learned via GP regression on descriptors, enabling location-adaptive uncertainty. Materials far from training distributions receive appropriately inflated variances, preventing overconfident extrapolation.

Computational efficiency is achieved through: - Cluster-based subsampling: Evaluate likelihood on representative materials per cluster - Importance sampling: Focus on materials where top potentials disagree most strongly - Online updating: Sufficient statistics for recursive posterior revision

2.2.2 Bayesian Information Criterion Approximations for Large-Scale Comparison

| Criterion | Formula | Assumptions | GLIM Applicability |
| --- | --- | --- | --- |
| BIC | −2log L + d_k log n | Large n, unimodal posterior | Excellent (n=12,000) |
| AICc | −2log L + 2d_k n/(n−d_k−1) | Small-sample correction | Moderate (d_k << n) |
| WAIC | −2Σ_i log E_θ[p(y_i¦θ)] + 2Σ_i Var_θ[log p(y_i¦θ)] | Posterior variance matters | Good for MLIAPs |
| LOO-CV | Σ_i log p(y_i¦y_{−i}) | Computationally intensive | Gold standard, sampled |

Table 9: Information criteria for marginal likelihood approximation, with applicability to GLIM-scale benchmarks.

BIC is primary for GLIM due to large n, but WAIC and LOO-CV provide sensitivity analysis for complex MLIAPs where effective parameter count is ambiguous. Empirical calibration against held-out performance validates criterion selection.

2.2.3 Stochastic Search Variable Selection for High-Dimensional Model Spaces

SSVS explores 2^23 ≈ 8 million possible subsets via MCMC sampling of binary inclusion indicators γ_k. The joint prior p(γ) = ∏_k π_k{γ_k}(1−π_k){1−γ_k} encodes inclusion beliefs, with Gibbs sampling updating each γ_k given others.

Hierarchical extensions group potentials by family (EAM, MEAM, NN, etc.), encouraging diverse-type selection over many similar variants. Material-adaptive SSVS makes γ_k depend on descriptors: different potentials for different material classes.

2.3 Advanced BMA Extensions

2.3.1 Hierarchical BMA for Structured Potential Families

The 23 GLIM potentials cluster into families with shared methodology. Hierarchical BMA models performance at multiple levels:

θkf=μf+δk, δk∼N0,τf2

where μ_f is family mean, δ_k is potential-specific deviation, and τ_f² controls shrinkage strength. This borrows strength across family members: rare potentials inform from relatives, with adaptive regularization—strong shrinkage for similar potentials, weak for diverse families.

2.3.2 Dynamic BMA with Online Model Updating

Sequential Bayesian updating revises posteriors as new DFT data arrives:

pt+1Mk∝pyt+1|Mk,mt+1⋅ptMk

Forgetting factors downweight old data for non-stationary environments where potential performance evolves. Change-point detection triggers model updates when prediction errors systematically deteriorate, indicating concept drift.

2.3.3 Connection to Stacking and Super-Learning Approaches

| Method | Weight Learning | Uncertainty | When Preferred |
| --- | --- | --- | --- |
| BMA | Marginal likelihood | Full predictive distribution | Model correctness assumed |
| Stacking | Cross-validation | Bootstrap/approximate | Model misspecification likely |
| Super-learning | Arbitrary meta-learner | CV-based | Complex interaction patterns |
| Pseudo-BMA | Stacking weights with BMA form | Hybrid | Practical compromise |

Table 10: Comparison of ensemble combination methods, showing complementary strengths.

Stacking often outperforms BMA empirically when the true model is outside the candidate set, but provides less reliable uncertainty. Hybrid approaches (BMA weights with stacking recalibration) combine theoretical coherence with empirical robustness.

3. Acquisition Functions for Potential-Specific Trust Assignment

3.1 Information-Theoretic Acquisition Strategies

3.1.1 Predictive Entropy Search for Minimum Error Location

Predictive Entropy Search (PES) selects evaluations to maximize expected reduction in entropy over the optimal potential’s location. For material m and potential k:

αPESm,k=Hk*|D−Ey∼py|m,k,DHk*|D∪{m,k,y}

where k* = argmin_k E[(y_true − ŷ_k)²] is the optimal potential. PES targets decision-relevant uncertainty: materials where multiple potentials appear competitive and predictions are uncertain receive highest priority.

Computational challenges: PES requires integration over posterior distributions, addressed via expectation propagation or Monte Carlo approximation. For GP surrogates, efficient approximations exploit analytic predictive forms. Batch PES extends to parallel evaluation, with greedy selection and submodularity guarantees ensuring near-optimal diversity.

3.1.2 Max-Value Entropy Search for Best Potential Identification

Max-Value Entropy Search (MES) targets reduction in entropy of the maximum achievable accuracy:

αMESm,k=Hy*|D−EyHy*|D∪{m,k,y}

where y* = min_k E[(y_true − ŷ_k)²]. MES is appropriate when any accurate prediction suffices, regardless of which potential provides it. This differs from PES: MES values achieving high performance; PES values knowing which potential achieves it.

Computational advantages: The maximum value is scalar, simplifying entropy calculations versus vector-valued location in PES. For 23 potentials, exact MES is feasible with numerical integration or sampling methods.

3.1.3 Joint Entropy Reduction Across Material-Property Space

Full uncertainty in GLIM is joint across materials, properties, and potentials. Joint Entropy Reduction (JER) targets:

αJERm,k,p=HF|D−EypHF|D∪{m,k,yp}

where F is the full performance tensor and p indexes properties (K, C’, C44).

PCA-based approximation: With 55% variance in PC1, low-rank factorization F ≈ UVᵀ + E reduces effective dimensionality. JER on latent factors U, V enables scalable computation. Greedy decomposition via chain rule: H[F] = H[f_1] + H[f_2|f_1] + … prioritizes most informative materials first.

3.2 Uncertainty-Aware Acquisition Design

3.2.1 Upper Confidence Bound Formulations with Ensemble Variance

Upper Confidence Bound (UCB) balances predicted performance with uncertainty:

αUCBm,k=−μkm+βσk2m+σensemble2m

where σ²_ensemble(m) = Var_k[μ_k(m)] is cross-potential variance, capturing epistemic uncertainty about which potential is correct.

| β Selection | Theoretical Basis | Practical Implementation |
| --- | --- | --- |
| √(2 log t) | UCB1 regret bound | Standard, may over-explore early |
| √(2 log(t^{d/2+2}π²/3δ)) | Finite-time guarantee | Confidence parameter δ |
| Adaptive: β_t = β_0/t^γ | Annealing exploration | γ = 0.5 typical, validated |
| Empirical Bayes | Maximize held-out reward | Cross-validation on GLIM |

Table 11: β selection strategies for UCB, balancing theoretical guarantees with practical performance.

Heteroscedastic UCB accommodates input-dependent noise: σ²(m) = σ²_GP(m) + g(m) where g(m) is learned variance function. Materials with high noise but low signal are appropriately deprioritized.

3.2.2 Expected Improvement with Heteroscedastic Noise Models

Expected Improvement (EI) quantifies expected reduction in error:

αEIm,k=Emax0,f*−fm,k|D=σmzΦz+ϕz

where **z = (μ(m) − f*)/σ(m), Φ and φ are standard normal CDF/PDF**.

Heteroscedastic extension: σ²(m) = σ²_GP(m) + σ²_noise(m) with learned noise function. Materials with systematically larger errors (complex oxides, high-entropy alloys) receive appropriate uncertainty inflation, preventing overconfident selection.

3.2.3 Knowledge Gradient for Correlated Potential Evaluations

Knowledge Gradient (KG) accounts for information propagation through correlations:

αKGm,k=ED′maxk′μk′(m′D′)D−maxk′μk′m′|D

where D’ = D ∪ {(m, k, y)}. The correlation structure from GLIM PCA—55% variance in PC1—means evaluating one potential informs others. Multi-output GP with coregionalization kernel:

Km,k,m′,k′=kmm,m′⊗kkk,k′

enables efficient KG computation via Kronecker structure.

3.3 Multi-Potential Query Strategies

3.3.1 Thompson Sampling for Potential Selection

Thompson Sampling implements probability matching: sample θ ~ p(θ|D), then select k = argmax_k θ_k. This automatically balances exploration and exploitation without tuning: uncertain potentials have high sampling variance and are occasionally selected; high-performing potentials have concentrated posteriors and are frequently selected.

| Variant | Posterior Representation | Computational Cost | Regret Bound |
| --- | --- | --- | --- |
| Standard TS | Exact Gaussian | O(K²) per decision | O(√(KT log T)) |
| Linear TS | θ_k = xᵀβ_k | O(d²K) | O(d√(KT)) |
| GP-TS | Function space sampling | O(n³) approximate | O(γ_T √T) |
| Batch TS | Parallel independent samples | O(bK²) for batch size b | O(√(KT/b)) |

Table 12: Thompson Sampling variants for potential selection, with computational and statistical properties.

For GLIM: GP-TS with 23 potentials is tractable with sparse approximations. Batch TS enables parallel DFT evaluation with diversity from sampling stochasticity.

3.3.2 Multi-Armed Bandit Formulations with Correlated Arms

Contextual bandits extend to material-feature-dependent rewards: E[r_k|m] = f_k(φ(m)) where φ(m) are descriptors. Linear contextual bandits: f_k(φ) = φᵀθ_k. GP contextual bandits: f_k ~ GP(0, k_k) with kernel over material space.

Correlation structure from GLIM: 55% PC1 variance suggests low effective dimensionality, enabling efficient learning. Kernelized bandits achieve regret scaling with effective dimension rather than raw material count.

3.3.3 Gittins Indices for Sequential Potential Allocation

Gittins indices provide optimal discounted infinite-horizon policies. For potential k, the index is maximum discount rate where k is preferred to safe alternative. Computational challenges: requires dynamic programming, addressed via Whittle index approximation or Monte Carlo tree search.

Finite-horizon GLIM applications: rollout policies approximate lookahead value, with batch KG providing practical alternative.

4. Active Learning with Model Disagreement Uncertainty

4.1 Query-by-Committee for Interatomic Potentials

4.1.1 Vote Entropy Across 23-Potential Predictions

Query-by-Committee (QBC) leverages ensemble disagreement to identify informative materials. For discretized predictions into bins b:

Hvotem=−b​nbm23lognbm23

where n_b(m) is the count of potentials predicting bin b. Maximum entropy (uniform distribution) indicates strongest disagreement and highest information value.

| Disagreement Measure | Formula | Computational Cost | Best For |
| --- | --- | --- | --- |
| Vote entropy (binned) | −Σ_b (n_b/K) log(n_b/K) | O(K) | Discrete decisions, interpretability |
| Empirical variance | (1/(K−1)) Σ_k (ŷ_k − ŷ̄)² | O(K) | Continuous predictions, simplicity |
| Average KL divergence | (1/K²) Σ_{i,j} D_KL(p_i¦¦p_j) | O(K²) | Probabilistic predictions, full distribution |
| Mutual information | I(θ; y¦m) | O(K) with approximations | Information-theoretic rigor |

Table 13: Disagreement measures for QBC, with computational and applicability considerations.

For continuous elastic constants: empirical variance or kernel density-based entropy substitutes for discrete vote entropy. Materials with σ²_ensemble > threshold are prioritized for DFT validation.

4.1.2 Average KL Divergence for Continuous Property Predictions

For probabilistic predictions p_k(y|m), the average pairwise KL divergence:

DKLm=1K2i,j​DKLpi⋅|m∥pens⋅|m

where p_ens = (1/K) Σ_k p_k is the mixture distribution. This captures both mean and variance disagreement, identifying materials where potentials differ in confidence as well as point estimates.

4.1.3 Committee Variance as Proxy for Epistemic Uncertainty

Committee variance provides the simplest, most widely used disagreement measure:

σcommittee2m=1K−1k​ykm−ym2

Decomposition: Total error² = Bias² + σ²_committee + σ²_aleatoric. The committee variance term is reducible epistemic uncertainty—target of active learning.

Calibration assessment: Correlation of σ²_committee with held-out DFT error validates QBC effectiveness. For well-calibrated ensembles, high committee variance predicts high actual error.

4.2 Uncertainty-Driven DFT Prioritization

4.2.1 Maximum Expected Prediction Error (MEPE) Criteria

Maximum Expected Prediction Error (MEPE) prioritizes materials with highest expected squared error:

αMEPEm=μ2m+σ2m

combining systematic bias (μ) and uncertainty (σ). For GP surrogates, this has closed form with heteroscedastic extensions.

| MEPE Component | Source | Reduction Strategy |
| --- | --- | --- |
| μ²(m) | Systematic model bias | Model correction, ensemble centering |
| σ²_GP(m) | GP posterior variance | More data in neighborhood |
| σ²_noise(m) | Irreducible aleatoric noise | Accept or improve measurement precision |

Table 14: MEPE decomposition with targeted reduction strategies.

4.2.2 Bayesian Active Learning by Disagreement (BALD)

BALD maximizes mutual information between model parameters and predictions:

αBALDm=Hy|m,D−EθHy|m,θ

High BALD: potentials make confident but different predictions (high predictive entropy, low expected conditional entropy). Low BALD: potentials agree or are individually uncertain.

4.2.3 Expected Model Change for Potential Improvement

Expected Model Change (EMC) selects materials most altering the model if known:

αEMCm=Ey∥θ−θ+m,y∥

For GPs, high EMC corresponds to high posterior variance—materials where the surrogate is most sensitive to new data.

4.3 Pool-Based and Stream-Based Active Learning

4.3.1 Density-Weighted Uncertainty Sampling

Pure uncertainty sampling can target outliers with low relevance. Density-weighted uncertainty sampling corrects:

αDWUSm=σ2m⋅pmβ

| β Value | Effect | Use Case |
| --- | --- | --- |
| β = 0 | Pure uncertainty sampling | Exploration-focused, outlier detection |
| β = 1 | Uncertainty × density | Balanced, representative exploration |
| β > 1 | Strong density emphasis | Conservative, core distribution focus |
| β < 0 | Explicit outlier targeting | Robustness testing, anomaly detection |

Table 15: Density weighting exponent β and its effect on exploration characteristics.

4.3.2 Cluster-Based Representative Selection from JARVIS-FF

HDBSCAN clustering in PCA-reduced descriptor space identifies natural material groupings. Per-cluster uncertainty sampling ensures diversity: select most uncertain material from each cluster, proportional to cluster size and aggregate uncertainty.

Hierarchical structure: 2–3 clusters on PC1 (55% variance) for coarse partitioning; finer clustering on higher components for refined diversity.

4.3.3 Adaptive Subsampling for Computational Budget Constraints

Dynamic β annealing: β_t decreases as budget depletes, shifting from exploration to exploitation. Budget-aware acquisition: explicit cost integration in value-of-information calculation.

5. Multi-Fidelity and Multi-Objective Bayesian Optimization

5.1 Multi-Fidelity Gaussian Process Frameworks

5.1.1 Linear Autoregressive Coregionalization: Cheap Classical to Expensive ML Potentials

The multi-fidelity framework structures relationships between information sources of varying cost and accuracy. For interatomic potentials, the natural hierarchy is:

| Fidelity Level | Methods | Cost (s/atom) | Accuracy | Primary Use |
| --- | --- | --- | --- | --- |
| s=1 (Lowest) | EAM, MEAM, Lennard-Jones | ~10⁻⁵ | Moderate | Large-scale screening, MD |
| s=2 (Intermediate) | SNAP, GAP, MTP | ~10⁰–10¹ | Good | Targeted exploration, validation |
| s=3 (High) | Deep NN potentials (M3GNet, MACE) | ~10¹–10² | Very good | Accurate property prediction |
| s=4 (Highest) | DFT, experiment | ~10²–10⁴ | Reference | Ground truth, final validation |

Table 16: Multi-fidelity hierarchy for interatomic potential selection, with cost-accuracy trade-offs.

The linear autoregressive model (arXiv.org) :

fsx=ρs−1fs−1x+δsx

where ρ_{s−1} is the correlation coefficient and δ_s ~ GP(0, k_s) is the fidelity-specific residual. This enables information propagation: cheap s=1 evaluations inform expensive s=4 predictions through learned correlations.

Empirical validation: The GP-MFBO framework for temperature/humidity calibration achieved 81.7% improvement in temperature uniformity and 76.3% in humidity uniformity over baselines, with 94.2% confidence interval coverage (nih.gov) . These results transfer directly to potential selection: strategic use of cheap potentials reduces expensive DFT burden dramatically.

5.1.2 Nonlinear Multi-Fidelity GPs with Deep Kernel Learning

Linear coregionalization fails when fidelity relationships are input-dependent. Deep kernel learning addresses this:

fsx=GP0,ksgsx,gsx′

where g_s is a neural network feature extractor. Learned features identify material subspaces where fidelity correlations are strong, enabling adaptive fidelity selection.

5.1.3 Multi-Output GPs for Correlated Elastic Constants

Intrinsic coregionalization model (ICM) for K, C’, C44:

Km,p,m′,p′=kmm,m′×Bp,p′

where B is 3×3 coregionalization matrix learned from GLIM data. Strong K–C44 correlations in metals, weaker C’ correlations in covalent systems are automatically captured.

5.2 Cost-Aware Acquisition Functions

5.2.1 Expected Improvement per Unit Cost

αEI/Cm,s=Emax0,fs*−fsmcs

Normalizes information gain by computational cost, automatically favoring cheap evaluations when informative. For GLIM’s 10⁹ cost ratio, EI/C front-loads classical potential screening before selective DFT validation.

5.2.2 Knowledge Gradient with Budget Constraints

KGCB optimizes long-term value given total budget B:

αKGCBm,s=1csEValue of information from m,s for optimal allocation of remaining B−cs

Nested optimization is computationally demanding; rollout approximations enable practical implementation.

5.2.3 Look-Ahead Acquisition for Sequential Cost-Benefit Analysis

Two-step look-ahead: simulate how cheap evaluation informs subsequent expensive decision. For GLIM: Does EAM evaluation justify ML potential query, or escalate directly to DFT?

5.3 Multi-Objective Pareto Optimization

5.3.1 Expected Hypervolume Improvement for Accuracy-Cost Trade-offs

EHVI quantifies expected increase in dominated hypervolume:

αEHVIm,s=EHVP∪{m,s}−HVP

where P is current Pareto set and HV is hypervolume indicator. For 23 potentials × 3 properties × cost, EHVI identifies evaluations expanding optimal trade-off frontier.

5.3.2 ParEGO for Scalarized Multi-Objective Potential Selection

ParEGO randomizes scalarization weights λ ~ Dirichlet(α):

fλm,s=λ1⋅AccuracyK+λ2⋅AccuracyC′+λ3⋅AccuracyC44+λ4⋅−Cost

Sequential scalarization with standard EI approximates full Pareto frontier without explicit multi-objective optimization.

5.3.3 Multi-Objective Information-Theoretic Acquisition

Pareto entropy search targets reduction in entropy of Pareto set location. Computationally demanding but theoretically principled for comprehensive trade-off exploration.

5.4 Adaptive Fidelity Selection

5.4.1 Fidelity-Aware Entropy Search

Joint selection of fidelity and location:

αFESm,s=Iθ;ym,s|Dcs

Information gain per unit cost automatically determines optimal fidelity level.

5.4.2 Multi-Information Source Optimization

Non-hierarchical fidelity structure: different potentials excel for different material classes. MISO learns source reliability from historical performance, adaptively selecting best source per query.

5.4.3 Online Fidelity Ranking from GLIM Performance Data

Bayesian updates to fidelity correlations: as new (m, s, y) tuples arrive, posterior over ρ_{s,s’} and δ_s functions revises. Rapid adaptation to discover unexpectedly informative cheap sources.

6. Batch Active Learning for High-Dimensional Experimental Design

6.1 Batch Mode Uncertainty Quantification

6.1.1 Local Penalization for Diverse Batch Selection

Sequential selection with distance penalty:

αpenalizedm=αm⋅mi∈batch​ϕ∥m−mi∥

where φ decays with descriptor space distance. Ensures batch diversity without explicit combinatorial optimization.

6.1.2 Determinantal Point Processes for Repulsive Sampling

DPP probability: p(S) ∝ det(K_S) where K is similarity kernel. Naturally balances quality (high α) with diversity (low similarity). Efficient sampling via eigendecomposition.

6.1.3 Thompson Sampling with Correlated Batch Rewards

Parallel TS samples: K independent θ^(b) ~ p(θ|D), select m_b = argmax_m θ^(b)·f(m). Correlation through shared posterior ensures diversity without explicit penalty.

6.2 High-Dimensional Composition and Structure Spaces

6.2.1 Additive Gaussian Processes for Compositional Inputs

Decomposition: f(composition, structure) = f_comp(composition) + f_struct(structure) + f_interact(composition, structure). Reduces sample complexity and improves interpretability.

6.2.2 Deep Kernel Learning with Structural Descriptors

SOAP/ACSF descriptors → neural network → GP kernel. Learned invariances (rotation, permutation, translation) built into structural fingerprints.

6.2.3 Random Embedding Bayesian Optimization for Latent Spaces

Random projection to d_eff-dimensional subspace where d_eff << d_raw. Effective dimensionality from GLIM PCA: 2–3 dimensions capture ~70% variance.

6.3 Parallel and Distributed Acquisition

6.3.1 Constant Liar Strategies for Asynchronous Evaluation

Impute pending results with constant value (mean or optimistic). Enables continued selection without waiting for stragglers. “Lie” corrected when true value arrives.

6.3.2 Kriging Believer for Pending Observations

Impute with GP posterior mean: more informed than constant liar. Accounts for expected information content of pending evaluations.

6.3.3 Rollout Acquisition for Long-Horizon Planning

Simulate future sequences: evaluate value of current decision under optimal continuation. Computationally intensive; limited lookahead (2–3 steps) often sufficient.

7. Gaussian Process Surrogates for Potential Error Prediction

7.1 GP Architectures for Error Surrogates

7.1.1 Standard GP Regression with Matérn and RBF Kernels

| Kernel | Smoothness | Computational Cost | Best For |
| --- | --- | --- | --- |
| RBF (squared exponential) | Infinitely differentiable | O(n³) | Smooth, well-behaved landscapes |
| Matérn-3/2 | Once differentiable | O(n³) | Moderate irregularity |
| Matérn-5/2 | Twice differentiable | O(n³) | Recommended default for materials |
| Rational quadratic | Mixture of length scales | O(n³) | Multi-scale phenomena |

Table 17: Kernel selection for GP surrogates in materials applications.

Matérn-5/2 recommended: balance between smoothness and flexibility, avoiding overconfident extrapolation of RBF.

7.1.2 Heteroscedastic GPs for Input-Dependent Noise

Twin GP formulation: mean function μ(m) and log-variance function log σ²(m) each modeled with independent GPs. Joint optimization via variational inference or expectation propagation.

7.1.3 Warped GPs for Non-Gaussian Error Distributions

Parametric warping: y → Φ(y) where Φ is sinh-arcsinh or similar transformation. Heavy-tailed errors (occasional catastrophic failures) better modeled with appropriate warping.

7.2 Feature Engineering for Material Representation

7.2.1 Compositional Descriptors: Magpie, Oliynyk, and Modified Pettifor Scales

| Descriptor Set | Features | Coverage | Best For |
| --- | --- | --- | --- |
| Magpie | 145 elemental properties + statistics | All inorganic compositions | General-purpose screening |
| Oliynyk | Ionic radii, electronegativity differences | Ionic/covalent systems | Structure prediction, stability |
| Modified Pettifor | Single-number chemical scale | Periodic trends | Bonding classification, similarity |

Table 18: Compositional descriptor sets for materials representation.

7.2.2 Structural Fingerprints: SOAP, ACSF, and Moment Tensor Descriptors

| Fingerprint | Invariance | Completeness | Computational Cost |
| --- | --- | --- | --- |
| SOAP | Rotation, translation, permutation, reflection | Complete basis | Moderate (O(n_atoms × n_species)) |
| ACSF | Same as SOAP | Hand-designed, incomplete | Fast (precomputed functions) |
| Moment tensors | Rotation, translation, permutation | Polynomial-complete | Moderate |

Table 19: Structural fingerprints for local atomic environment description.

7.2.3 Learned Representations from Crystal Graph Convolutional Networks

CGCNN, MEGNet, ALIGNN: end-to-end learned embeddings from crystal graphs. Pre-trained on large databases, fine-tuned on GLIM benchmark. Task-specific representations may outperform hand-engineered features.

7.3 Uncertainty Calibration and Validation

7.3.1 Probability Integral Transform for Calibration Assessment

PIT histogram: uniform for well-calibrated predictions. U-shaped: underconfidence; inverse-U: overconfidence. Recalibration via temperature scaling or isotonic regression.

7.3.2 Conformal Prediction for Distribution-Free Uncertainty

Coverage guarantee: P(y_true ∈ C_α(x)) ≥ 1−α for any distribution, any model. Split conformal: efficient, valid with exchangeability.

7.3.3 Cross-Validation Strategies for Large-Scale Benchmarks

| CV Strategy | Structure | Use Case |
| --- | --- | --- |
| Random | Shuffle all data | Optimistic, assesses interpolation |
| Leave-one-material-out | Hold out single material | Realistic generalization |
| Leave-one-cluster-out | Hold out material cluster | Extrapolation to new classes |
| Time-based | Train on older, test on newer | Temporal generalization |

Table 20: Cross-validation strategies for GLIM-scale benchmarks.

7.4 Scalable GP Approximations

7.4.1 Sparse Variational GPs with Inducing Points

Variational lower bound: O(nm²) for m << n inducing points. Optimization of inducing locations and kernel parameters jointly. Modern implementations: millions of data points.

7.4.2 Random Fourier Features for Kernel Approximation

Explicit feature map: k(x,x’) ≈ φ(x)ᵀφ(x’) with φ(x) = [cos(w_iᵀx + b_i)]. Primal space regression: O(nd²) for d features, efficient when d << n.

7.4.3 Neural Network-Based Mean Functions for Complex Error Landscapes

Deep network mean + GP residual uncertainty: f(x) = NN(x) + δ(x) where δ ~ GP(0, k). Combines representation learning with calibrated uncertainty.

8. Applicability Domain Methods from QSAR/Cheminformatics

8.1 Distance-Based Domain Characterization

8.1.1 Leverage Statistics in Descriptor Space

Leverage: h_i = x_iᵀ(XᵀX)⁻¹x_i. High h_i: extrapolative relative to training data. Warning threshold: h_i > 3p/n typically.

8.1.2 Hotelling’s T² for Multivariate Outlier Detection

T² = (x−μ̄)ᵀS⁻¹(x−μ̄). Accounts for feature correlations. Extreme values: underrepresented regions where predictions unreliable.

8.1.3 k-Nearest Neighbor Distance in Feature Space

Nonparametric density proxy: large distance to k-th nearest neighbor indicates low training density. Adaptive k based on local density variation.

8.2 Density-Based and Probabilistic Approaches

8.2.1 Kernel Density Estimation for Training Set Distribution

KDE: p̂(x) = (1/n) Σ_i K_h(x−x_i). Bandwidth h: cross-validated or rule-of-thumb. Low p̂(x): domain violation.

8.2.2 One-Class SVM for Novelty Detection

Decision boundary enclosing training data. Kernel and regularization control boundary tightness. Trade-off: false positives vs. false negatives.

8.2.3 Gaussian Mixture Models for Multi-Modal Domains

Multi-modal training distribution: materials cluster into distinct classes (metals, oxides, semiconductors). GMM captures this structure, flagging low-probability regions.

8.3 Ensemble-Based Domain Definitions

8.3.1 Standard Deviation of Ensemble Predictions

σ_ensemble(x): natural applicability domain measure. No explicit descriptor construction required. High σ: ensemble uncertain, domain boundary likely.

8.3.2 Bootstrap Aggregation Confidence Intervals

Empirical distribution across bootstrap samples. Narrow intervals: reliable predictions; wide intervals: uncertain, near boundary.

8.3.3 Conformal Prediction Sets for Coverage Guarantees

Explicit error rate control: (1−α) coverage guaranteed. For potential selection: rigorous statements about trustworthiness.

8.4 Adaptation to Materials-Specific Challenges

8.4.1 Composition-Structure-Property Relationship Modeling

Non-unique mapping: similar compositions → different structures → different properties. Joint modeling of composition→structure→property required for reliable domain definition.

8.4.2 Transferability Across Crystal Systems and Chemistries

Critical challenge: potential trained on fcc metals fails for hcp or bcc. Explicit crystal system indicators or learned representations must detect such boundaries.

8.4.3 Dynamic Domain Updating with Active Learning

Conservative initial domain, relaxed as confidence grows. Explicit tracking of domain expansion vs. exploitation of known regions.

9. GLIM-Style Meta-Analysis: Practical Implementation

9.1 Exploratory Data Analysis of Potential Performance

9.1.1 Performance Clustering via PCA and t-SNE

PCA: 55% variance in PC1 → global quality axis. t-SNE/UMAP: nonlinear clustering revealing fine-grained structure. Materials with similar potential rankings cluster together → transfer of selection decisions.

9.1.2 Correlation Structure Across Elastic Constants

| Property Pair | Typical Correlation | Bonding Type Dependence |
| --- | --- | --- |
| K–C44 | Strong positive | Metallic systems |
| K–C’ | Moderate | Variable by structure |
| C’–C44 | Weak to moderate | Strongest in covalent systems |

Table 21: Elastic constant correlations and their bonding-type dependence.

9.1.3 Systematic Error Patterns by Material Class

Regression analysis: potential error ~ material class indicators. Quantified patterns: EAM excellent for simple metals, fails for oxides; MLIAPs more consistent but slower.

9.2 Meta-Learning for Potential Recommendation

9.2.1 Learning to Learn: Feature-Based Meta-Models

Meta-model: predict best potential from material descriptors. Training: GLIM performance matrix. Zero-shot generalization to new materials.

9.2.2 Prototypical Networks for Material-Potential Matching

Prototype per potential: mean embedding of materials where it excels. New material: classify to nearest prototype. Interpretable, uncertainty via distance.

9.2.3 Graph Neural Networks for Relational Potential Ranking

Bipartite graph: materials ↔ potentials with performance edges. Message passing: embed materials and potentials jointly. Link prediction: unobserved performance estimation.

9.3 Online Decision Frameworks

9.3.1 Contextual Bandits for Material-Adaptive Selection

Linear/Neural contextual bandits: reward(potential|material features) learned online. Regret bounds: sublinear growth, asymptotic optimality.

9.3.2 Bayesian Optimization with Meta-Priors from GLIM

Strong prior from benchmark: rapid convergence for new materials. Warm start: posterior concentrated near GLIM-informed values.

9.3.3 Regret Bounds and Asymptotic Optimality Guarantees

Theoretical justification: GP-UCB, Thompson Sampling achieve O(√(γ_T T)) regret. γ_T: maximum information gain, depends on kernel and dimensionality.

10. Integration and Practical Implementation Guidance

10.1 Software Ecosystem and Tools

| Tool | Purpose | Key Features | Integration |
| --- | --- | --- | --- |
| BoTorch/GPyTorch | Modern Bayesian optimization | GPU acceleration, auto-diff, modular acquisitions | Primary framework |
| scikit-learn/GPy | Classical GP implementations | Accessible, stable, well-documented | Prototyping, education |
| ASE | Atomistic simulation | Unified calculator interface, MD engines | Potential evaluation |
| pymatgen | Structure manipulation | Crystal analysis, I/O, builders | Descriptor computation |
| Matminer | Feature extraction | Magpie, SOAP, structure featurizers | Pipeline integration |
| AiiDA/FireWorks | Workflow orchestration | Provenance, distributed execution | Scale-out deployment |

Table 22: Software ecosystem for Bayesian optimization of interatomic potential selection.

10.2 End-to-End Workflow Design

10.2.1 Offline Preprocessing: GLIM Benchmark Ingestion and Feature Computation

One-time cost: descriptor computation, similarity matrices, meta-model training. Cached representations accelerate online decisions.

10.2.2 Online Decision Loop: Query, Evaluate, Update, Recommend

Input: Material m with descriptors φ(m)
1. Predict: μ_k(m), σ_k(m) for all k potentials via GP surrogate
2. Select: (m, k*) = argmax acquisition(μ, σ, cost)
3. Evaluate: Run potential k* on material m, observe y
4. Update: Incorporate (m, k*, y) into GP posterior
5. Recommend: Return best predicted potential or BMA prediction

10.2.3 Human-in-the-Loop Validation for Critical Applications

Expert override: uncertainty estimates, similar materials, known failure modes presented for review. Feedback improves future automation.

10.3 Validation and Benchmarking Protocols

10.3.1 Leave-One-Material-Out Cross-Validation

Primary metric: generalization to new materials. Correlation of predicted vs. actual best potential.

10.3.2 Time-Based Splits for Temporal Generalization

Training on older benchmark versions, testing on newer. Detects obsolescence as potentials improve.

10.3.3 Adversarial Testing for Robustness Assessment

Deliberately challenging materials: extreme compositions, unusual structures, engineered outliers. Stress testing reveals failure modes.

10.4 Future Directions and Open Challenges

10.4.1 Foundation Models for Universal Potential Pre-Training

Large-scale pre-training on diverse materials data → strong priors reducing need for material-specific selection. Uncertainty quantification and domain adaptation remain critical.

10.4.2 Causal Inference for Mechanistic Understanding

Beyond correlation: identify why potentials fail. Structural causal models guide targeted improvement rather than black-box selection.

10.4.3 Federated Learning for Distributed Potential Development

Multi-institutional collaboration without centralizing proprietary data. Bayesian methods naturally handle heterogeneous, incomplete information.